## Slide 1
NCRAPS-2023
5th National Conference on "Recent Advancement in Physical Sciences”
Organized by
National Institute of Technology, Uttarakhand
December 19-20, 2023
Paper ID: CHY-03
Development of Superhydrophobic/Oleophilic Fabric using Modified Nanotitania for Oil-water Separation
Presented by
Adeeba
Department of Chemistry Graphic Era (deemed to be) University
Dehradun, Uttarakhand

## Slide 2: CONTENTS
BACKGROUND
INTRODUCTION
AIMS AND OBJECTIVE
MATERIALS AND METHODS
RESULTS AND DISCUSSION
CONCLUSION

## Slide 3: Background
Sources of Oil Pollution
Textiles industries
Food industries
Petrochemicals industries
Mining industries
Chart: 
| Allision/ Collision | Grounding | Hull Failure | Equipment Failure | Fire/Explosion | Other
Column1 | 30 | 32 | 13 | 4 | 11 | 13
13%
4%
11%
13%
32%

## Slide 4: INTRODUCTION
Major effects of oil spills.
Human Health
Marine Eco system including animal and plant life
Damage beaches, Marshlands, and Fragile aquatic ecosystems
Recreational and commercial fisheries
Tourism
Toxicity
2

## Slide 5: TECHNOLOGIES AVAILABLE FOR OIL WATER SEPARATION
TECHNOLOGIES
DISTILLATION
FLOTATION TECHNOLOGY
SETTLING TANKS
INDUSTRIAL FILTRATION
SKIMMERS
CENTRIFUGATION
MEMBRANE SEPARATION
3

## Slide 6: SUPERHYDROPHOBIC/ SUPEROLEOPHILIC COATINGS
Advantages of these coatings in separation of oil water
Enhanced selectivity
Reduced Fouling
Increased Efficiency
Improved oil recovery
Environmental friendly
Fabric
Oil
Water

## Slide 7: WHY SOL-GEL METHOD?
Versatility
Customization of Surface Chemistry
Cost Effectiveness
Durability and stability
Resistance to fouling
Easy Implementation
Selective Affinity
4

## Slide 8: SOL: TITANIA ()
Photocatalytic activity
High surface area
Hydrophobicity
Enhanced Wettability control
Durability and Stability
Flexibility in Fabric Choice
Potential for Self-heating coatings
Simple application process
5

## Slide 9: MODIFICATION OF SOL WITH STEARIC ACID
STRUCTURE
octadecanoic acid
PROPERTIES
Biodegradable
Low Volatility (69.3 °C)
Thickening agent
Hydrophobic Nature
Advantages of Magnetite Chitosan composite
Synergistic Effect
Enhanced Stability and Durability
Film formation
Enhanced Hydrophobicity
Improved Oleophilicity
Biocompatibility and Biodegradability
Versatility
Adhesion to Fabric
6

## Slide 10: AIM AND OBJECTIVES
AIM: To prepare a Sol for separation of Oil-Water
1
Preparation of Titania Sol and hydrophobic modification using different ratios of stearic acid
2
Characterization of Sol solution using PSA, IR
3
Study of Oil-water separation efficiency
Study of Oil-Water separation efficiency

## Slide 11: Method for preparation of Titania Sol Solution and its Modification
Method adopted: Sol-gel method via Acid hydrolysis
Steps involved:
Fig1 : Preparation and modification of titania sol
11
- - - - - - -
- - - - - - -
- - - - - - -
- - - - - - -
Distilled Water
+
Ethanol
- - - - - - -
- - - - - - -
- - - - - - -
- - - - - - -
Acetic acid
+
Ethanol
- - - - - -
- - - - - -
- - - - - -
- - - - - -
TTIP
+
Ethanol
Magnetic Stirrer
Acified TTIP/
Ethanol Solution
- - - - - -
- - - - - -
- - - - - -
- - - - - -
Magnetic Stirrer
- - - - - -
- - - - - -
- - - - - -
- - - - - -
Magnetic Stirrer
Titania Sol
- - - - - - -
- - - - - - -
- - - - - - -
- - - - - - -
Stearic Acid
+
Ethanol
- - - - - -
- - - - - -
- - - - - -
- - - - - -
Modified Titania Sol
For 15 mins
For 3 hours
For 2 days

## Slide 12: Coating on Fabric
Dip coating method
12
Fig 2: Schematic representation of coating of nano-sol solution on fabric substrate
Hydrophobically modified nanostructured fabric
Modified Titania Sol
Uncoated fabric
Coating on fabric

## Slide 13: CHARACTERIZATION

## Slide 14: Particle Size Analysis (PSA)
RESULTS REVEAL THAT:
Size is 39.5 nm
Polydispersity Index is 0.725
Fig 3: PSA of Titania sol

## Slide 15: FE-SEM ANALYSIS
RESULTS REVEAL THAT:
Roughness
Every single thread is coated
Nano sized 30-40 nm approximately
Fig 4: FE-SEM images of Uncoated and Coated fabric
13
Uncoated Fabric
Coated
Fabric

## Slide 16: FE-SEM EDX ANALYSIS
C K
N K
O K
Ti K
a
C K
N K
O K
Ti K
b
Fig 5: a) is showing the FE-SEM EDX of uncoated fabric
b) is showing the FE-SEM EDX of coated fabric

## Slide 17: FTIR ANALYSIS
RESULTS ARE:
Peak at wavenumber () | Functional Group
3349 | O-H stretching
2273 | C-H strething
1632 | O-H bending
1399 | C-O vibration
672 | Ti-O vibration
663 | Ti-O vibration
 | Functional Group
3349 | O-H stretching
2273 | C-H strething
1632 | O-H bending
1399 | C-O vibration
672 | Ti-O vibration
663 | Ti-O vibration
Figure 6: FTIR spectra of Titania Sol
13

## Slide 18: Water Contact Angle (WCA)
RESULTS REVEAL THAT:
Contact angle is 163.3º
Showing superhydrophobicity
Uncoated fabric
Coated fabric

## Slide 19: OIL-WATER SEPARATION METHOD
Method Used
a
d
c
b

## Slide 20: OIL-WATER SEPARATION METHOD
Separation efficiency
KS= *100
Where,
Mi is initial mass of water
Mf is Final mass of water
KS is separation efficiency
97%
95%
92%
93%
94%
Toluene
Chloroform
Olive Oil
Coconut Oil
Sunflower Oil

## Slide 21: CONCLUSION
FTIR results revealed the successful fabrication of Titania Sol
Nano structured present on coated surface was confirmed by SEM
Superhydrophobicity of coated fabric was showing by WCA
97% is the highest oil separation efficiency of coated fabric for removal of chloroform.

## Slide 22
THANK YOU